Please provide the below information, and submit your “Abstract” with this “Abstract Information” to our 2026-ICGET-Tw Abstracts Submission System

| Abstract Information |  |
| --- | --- |
| Topic (Please select one from below): |  |
|  | (Topic 1) Batteries & Storage Devices |
|  | (Topic 2) Photoelectrochemistry & Solar Cells |
|  | (Topic 3) Conversions |
|  | (Topic 4) Basic Electrochemistry & Electroplating |
|  | (Topic 5) Bio & Chemical Sensors |
| Types of presentations (Please select one from below): |  |
|  | Oral (Note: Please be aware that each presentation will be 20 min including a 5 min period for questions and discussion.) |
|  | Oral Competition, if not available then poster competition |
|  | Poster |
|  | Poster Competition |

Poster for the 2026 ICGET-Tw

Poster Information

Size：A0 portrait format (841 mm wide × 1189 mm high)

Thanks for your cooperation!
Improved Electrochemical Performance of MOF-Derived Spinel NiCo2O4/SWCNT Composite as anode material for Na-ion Batteries

S. Kishore Babu and Wei-Ren Liu*

Department of Chemical Engineering, Chung Yuan Christian University, Taoyuan City, 320314, Taiwan

*Correspondence: wrliu@cycu.edu.tw

NSTC XXX-XXXX-X-XXX-XXX-MY3

# In this study, a MOF-derived NiCo2O4 spinel composite integrated with single-walled carbon nanotubes (SWCNT) was synthesized via a solvothermal process for advanced energy storage applications. The composite material demonstrates significantly enhanced electrochemical performance compared to bare NiCo2O4, particularly in sodium-ion battery applications. The rate capability results indicate that, at a current density of 0.1 A/g, the NiCo2O4/SWCNT composite exhibited an initial high reversible capacity of 862 mAh/g. After 100 cycles at a current density of 0.2 A/g, the NiCo2O4/SWCNT composite achieves a high reversible sodiation capacity of approximately 603 mAh/g. At the same time, bare NiCo2O4 exhibits only 337 mAh/g. Additionally, as the current density increases, the composite material continues to deliver outstanding performance, with reversible capacities of 369 mAh/g at 2 A/g and 252 mAh/g at 5 A/g. The exceptional performance was attributed to the synergistic effect of the SWCNT, which improved electron transport and structural stability; thus, NiCo2O4/SWCNT composites can be considered substantial anode materials for the next generation of sodium-ion batteries.

References

[1] J.-E. Zhou, R. C. K. Reddy, A. Zhong, Y. Li, Q. Huang, X. Lin, J. Qian, C. Yang, I. Manke, R. Chen, Metal–Organic Framework-Based Materials for Advanced Sodium Storage: Development and Anticipation. Adv. Mater. 2024, 36, 2312471.

[2] R. Li, Z. Long, C. Wu, H. Dai, W. Li, L. Bai, H. Qiao, K. Wang. Metal-organic frameworks-derived porous NiCo2O4/carbon composite nanofibers as anodes for Li/Na-ion batteries. J. Alloys Compd. 2023, 936, 168359.

The abstract should not be exceeded ONE PAGE of text, references, tables and figures. Abstracts exceeding this limit may be cut without consideration of content after the first page.

Type the title single-spaced in 14-point Times Roman bold, upper and lower case and

NOT in ALL CAPITAL letters.